TECHNICAL SPECIFICATION

Holographic Hot-stamping Foil

Design, required holographic elements:

- kinetic effect – color and achromatic

- flip-flop effect

- positive and negative microtext

- nanotext

- nanoimage, nanostructures

- lens effect

- color and achromatic bas-relief

- hidden 3D image

Non-registered motif (continuous design), motif must be seen from front side and back side after the application. Motif will be a partly metallized/demetallized.

The size of the applied hologram: 19 x 10 mm

Color: silver (front and back side)

Thickness: ca 19 um

Roll dimension:

Width of roll: 23 ± 0,5 mm

Winding on reel: 220 lm

Max. outside diameter of reel: 75 mm

Papercore: 1”

Application and substrate

Applied on a transparent polypropylene self-adhesive substrate

Applied on a STEUER (B2) hot stamping machine

Application temperature: 120°C - 170°C