Annex No. 1

TECHNICAL SPECIFICATION

SECURITY PAPER WITH EXCLUSIVE CONTINUOUS WATERMARK

Size: 	700 x 1000 mm

- combination of the long-grain (ca 40%) and short-grain (ca 60%) in one delivery

Grammage: 		100 g/m²

Composition: 	50% cotton and 50% chemical wood pulp

Characteristic: 	UV dull

Fibres: 		invisible, UV fluorescent green (length 6 mm, 50 pcs/dm² = the sum of both sides)

visible blue, UV fluorescent blue (length 6 mm, 50 pcs/dm² = the sum of both sides)

Watermark: 	continuous positive-negative exclusive watermark, the size of the repeating motif is

ca. 15x15mm

Printability: 		dry and wet offset, intaglio, hot stamping, numbering (letter press), laser printing

| CHARACTERISTIC | UNITS | SPECIFICATION | TOLERANCES | STANDARDS |
| --- | --- | --- | --- | --- |
| Grammage | g/m2 | 100 | Min 96, max 104 | DIN ISO 536 |
| Caliper (Thickness ) | µm | 120 | Min 110, max 130 | DIN EN 20534 |
| Opacity | % | 92 | Min 87, max 94 | DIN 53146 |
| Absolute humidity | % | 6 | Min 5, max 7 | ISO 287 |
| Reflectance R457 | % | 82 | Min 80, max 84 | ISO 53145 |
| Relative humidity | % | 50 | Min 45, max 55 |  |
| Surface rupture |  |  | Min 10 |  |
| Dennison wax |  |  |  |  |
| Cobb value | g/m2 | 25 | min 20, max 30 |  |