**TECHNICAL SPECIFICATION**

**(Physical properties)**

**Roll widths:** a) 170 mm, b) 180 mm, c) 195 mm, d) 210 mm

- a combination of different widths in one delivery in a minimum quantity of 2000 kg

**Grammage:** 70 g/m², 70 mm core inner diameter, maximum roll diameter 600 mm

**Composition:** waste paper can be used for production, which may contain different coloured visible fibres

and fluorescent fibers

**Printability:** white paper printable with flexo, water-based inks, the tapes produced from the material

are glued with DEXTRIN water-based adhesive.

|  |  |  |  |  |
| --- | --- | --- | --- | --- |
|  |  |  |  |  |
| **PROPERTY** | **UNIT** | **VALUE** | **TOLERANCE** | **STANDARD** |
| Grammage | g/m2 | 70 | +/- 4 % | ISO 536 |
| Moisture | % | 5 | min 4, max 7 | ISO 287 |
| Roughness | µm | 6 | min 5, max 7 | ISO 8791-4 |
| Cobb value | g/m2 | 25 | max 35 | ISO535 |
| Thickness | µm | 90 | +/- 4 % | ČSN EN 534 |