Annex No. 2

Encapsulation specification

Encapsulation specification of purchased chip modules

For the STARCOS cards:

- Supplier-Item-ID: SCOTV17.3G

- Type: DI_6

- Color: Gold

- Thickness: 600 µm

The inlay, the following material description:

SLAMs PVC 150μm with premium LOBRA coating 10g/m² (3x7) STC